| EASIPRENE |  |  | Technical Data Sheet |  |
| --- | --- | --- | --- | --- |
|  | Thermoplastic Elastomer (TPR) |  |  |  |

|  | EASIPRENE DB80385 |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Product Description |  |  |  |  |  |  |  |  |  |  |
|  |  | EASIPRENE ia a series of SBS (styrene-butadiene-styrene) or SEBS (Styrene-Ethylene-Butadiene-Styrene) type Thermoplastic Rubbers (Elastomers) that combine the properties of vulcanized rubber with the processing advantages of conventional thermoplastics. In other words, they allow the production of rubber-like articles using the fast processing equipment developed by the thermoplastics industries. |  |  |  |  |  |  |  |  |  |
|  | Processing Method |  |  |  |  | Other Information |  |  |  |  |  |
|  |  | Extrusion, Injection Molding |  |  |  |  | MetEN71-3；FDA 21CFR177.2600 aq. test |  |  |  |  |
|  | General Properties |  |  |  |  |  |  |  |  |  |  |
|  | Properties; Method; Values. Type; SBS. Colour; Visual; Natural. |
|  | Mechanical Properties |  |  |  |  |  |  |  |  |  |  |
|  | Properties; Method; Values. Hardness（5 sec delay）; Shore A; D2240; 80. Density; D792; 0.97. Elongation @Break; %; D412 – Die C; 321.8. Tensile Strenght; MPa; D412 – Die C; 10.87. 100% Modulus; MPa; D412 – Die C; 7.26. 300% Modulus; MPa; D412 – Die C; 10.67. Melt Flow Rate @5Kg/190oC; g/10min; D1238; 33.9. |
|  | Molding Properties |  |  |  |  |  |  |  |  |  |  |
|  | Molding Temperature; oC; Rear; 150 - 180. oC; Front; 160 - 190. oC; Nozzle; 170 - 190. Mold Temperature; oC; 25 - 40. Molding Parameters; speed; medium. kPa; Boost Pressure; 3500 - 5000. kPa; Back Pressure; 350 - 3000. Cooling Time; Sec.; 15-30. Drying Time and Temperature; No. |
| Issue Date: |  |  |  |  |  |  |  |  |  | March 2, 2006 |  |
|  |  |  |  | The properties shown are typical values and for are references only. The value should not be considered as limits to the specification. Since the conditions under which this material is used, are beyond our control, all suggestions and recommendations are without guarantee. |  |  |  |  |  |  |  |
|  |  |  | 梓金（香港）有限公司 Zhi Jin (Hong Kong) Company Limited |  |  |  |  |  |  |  |  |